REPAIRS TO RUBBER COMPONENTS

TR300		60 Fluid Elastomer

TR305		60 Paste Elastomer

TR310		60 Rapid Grade Elastomer

TR315		80 Fluid Elastomer

TR320		80 Paste Elastomer

TR 325		80 Brushing Elastomer

ELASTOMERIC REPAIR SYSTEMS - CHARACTERISTIC CHART

| Product Code | Product Name | Pack Size | Mixing Ratio | Usable Life (20C) | Cure Time | Machine Time | Coverage Rate per unit | Applied By | Max Temp Dry - Continuous Max Temp Wet - Continuous | Surface Prep - Degreased - Manual - Blasted |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TR300 | 60 Durometer Elastomer Fluid | 2 x 600gm | 2:1 | 25 mins | 3 hours | 16 hours | N/A | Brush | 120 | 80 | 80 | 50 | * |  | * |
| TR305 | 60 Durometer Elastomer Paste | 2 x 600gm | 2:1 | 25 mins | 3 hours | 16 hours | N/A | Spatula | 120 | 80 | 80 | 50 | * |  | * |
| TR310 | 60 Durometer Elastomer Rapid Grade | 10 x 125gm | 2:1 | 10 mins | 30 mins | 1 hour | N/A | Spatula | 120 | 80 | 80 | 50 | * |  | * |
| TR315 | 80 Durometer Elastomer Fluid | 2 x 600gm | 13:2 | 15 mins | 4 hours | 16 hours | N/A | Brush | 120 | 80 | 80 | 50 | * |  | * |
| TR320 | 80 Durometer Elastomer Paste | 2 x 600gm | 3:2 | 15 mins | 4 hours | 16 hours | N/A | Spatula | 120 | 80 | 80 | 50 | * |  | * |
| TR325 | 80 Durometer Elastomer Brush Grade | 1 x 3kg | 13:2 | 15 mins | 4 hours | 16 hours | 1.9sqm at 500 microns | Brush | 120 | 80 | 80 | 50 | * |  | * |

Max Temp Dry – maximum temperature when in contact with dry products ie – powders

Max Temp Wet – maximum temperature when in contact with wet products ie – water, sewage, chemicals

ELASTOMERIC REPAIR SYSTEMS

Use the table below to choose the right product for the application, then look at the following page for general characteristics on the product chosen. NOTE the table below is only a guide, if in doubt please contact our technical department for confirmation of the choice made

| Product Name | Cables | Castings | Conveyor Rebuild | Conveyor Coating | Gaskets | Hosing – Low Pressure Repair ++ | Moulds | Pump - Impeller | Tyre Repair – Off Road | Rapid Repairs Conveyor Hosing Tyres |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TR300 60 Durometer Paste | * |  | * |  |  | * |  |  | * |  |  |  |  |
| TR305 60 Elastomer Fluid |  |  |  | * |  |  |  |  | * |  |  |  |  |
| TR310 60 Durometer Rapid Grade Paste |  |  |  |  |  |  |  |  |  |  | * | * | * |
| TR315 80 Durometer Paste |  | * |  |  | * |  | * |  |  |  |  |  |  |
| TR320 80 Durometer Fluid |  | * |  |  | * |  | * |  |  |  |  |  |  |
| TR325 80 Durometer Brushing Grade |  |  |  |  |  |  |  | * |  |  |  |  |  |

REPAIRING FENDERS AND FLOATING HOSES

The following ThistleBond section is concerned with the repairing of Fenders and Floating Hoses and should be read in conjunction with the Technical Data sheets of the following ThistleBond Products: 60 Durometer Elastomer Paste and 80 Durometer Elastomer Paste.

## COMMON DEFECTS

Mechanical damage or wear.

## PREPARATION

All work should be carried out in strict accordance with the relevant ThistleBond Technical Data Sheet. Product selection and application should be based upon the nature and severity of the damage, the time available for work the system pressure and operating temperatures.

N.B. Repairs must not be attempted if damage to reinforcement layers is evident.

SURFACE PREPARATION

All loosely adhered material should be cut away and the repair area cut back using a sharp knife, this leaves a sound edge terminated square or undercut. Where exposed reinforcement fabric has become wet, it should be allowed to dry out. The complete area of damage and an area at least 3” around the damage should then be abraded to produce a woolly finish. This can be accomplished by using a rotary wire brush, or by the use of a roughing brush. Where metallic reinforcements are exposed, this should be thoroughly roughened and then washed with ThistleBond Universal Cleaner in order to remove all dirt, grease and other surface contaminants.

## PRIMING SYSTEM

Apply the ThistleBond Primer supplied with the product in a thin film to the entire prepared area, be sure to use a stiff bristled brush.

## APPLICATION TECHNIQUE

Mix the selected product and apply a thin layer to the prepared area. Ensure this layer of product is kept within the prepared area and is pushed will into the prepared profile. Wet out an appropriate length of ThistleBond reinforcement tape with the mixed product and apply this to the repair area. Where more then one length of reinforcement tape is required, ensure an overlap of a minimum of ¼” between lengths.

Finally, apply further product to totally encapsulate the reinforcement tape and in fill the repair area using a correctly contoured rigid applicator to re-profile the surface. If required a suitable rotary grinding tool can be used to finally contour the surface, after a full mechanical cure of the product has taken place.

TECHNICAL SUMMARY

##### PRODUCT			HARDNESS	WORKING 	FULL

##### LIFE (20°C	CURE	(20°C)

60 DUROMETER

ELASTOMER PASTE		60	25 MINUTES	     72 HOURS

80 DUROMETER

ELASTOMER PASTE		80	25 MINUTES	     72 HOURS

## MAIN SYSTEM SELECTION

## Required for High

## Abrasion Resistance		80 Durometer Elastomer Paste

## General Repair Work		60 Durometer Elastomer Paste